Time response of up-converted emission on cyanine dye J-aggregates
Y.Akutagawaa, K.Miyasuea, T.Sekiyaa, S.Kuritaa, M.Nakajimab, and T. Suemotob
aDepartment of Physics, Faculty of Engineering, Yokohama National University, Hodogaya-ku, Yokohama 240-8501, Japan
bInstitute for Solid State Physics, The University of Tokyo, Kashiwanoha, 5-1-5, Kashiwa-shi, Chiba 277-8581, Japan

[image: image1.wmf]d

r

t

t

e

e

I

t

I

t

t

/

/

0

)

1

(

)

(

-

-

-

=

It is well known that some dyes are able to form J-aggregates in aqueous solutions. The optical absorption spectra of the J-aggregates, exhibit a sharp band shifted to lower photon energy side from the monomer absorption band and called J-band. The J-band is due to the transition of excitons delocalized over the constituent molecules [1,2]. We observed an up-converted emmision band of J-aggregates of NK-2203 cyanine dye at 2.08 eV that was seen on high-energy side (0.12eV) than the excitation energy by He-Ne laser (1.96eV) [3]. This is not due to the two-photon absorption. The luminescence spectrum obtained by the low-energy excitation is quite similar to that by a band-to-band excitation. The mechanism of this up-converted emission of the J-band is of interest, so that time-resolved luminescence was investigated using tunable pulsed-laser systems. Figure 1 shows a decay curve of the J-band emission of 4×10-4 M aqueous solution measured by a forward scattering configuration with an excitation laser light operated at 2.00 eV. The line shape of the time-evolution depends on the excitation intensity. The time-evolution of the emission indicates that the emission maximum comes after a delay of a few picosecond from the excitation. We adopted a function, 
[image: image2.png]Tntensity [au]

7 T T
§ — 1 2,006V

---- fit_2.00eV
laser
T L L L
0 w0 w40

Time [ps]




, as representation of the decay curve. The resultant values of the rise time r and decay time d are about 3 ps and 200 ps, respectively. These are equivalent to those of the band-to-band excitation measured by the same condition. The temperature dependence of the up-converted luminescence intensity [4] suggests that the excitation and decay process in the luminescence is the same as that of the band-to-band excitation. This luminescence seems to be due to an optical excitation of thermally excited molecules in the aggregate. 
corresponding author e-mail:  sekiya@ynu.ac.jp
References
1. E. W. Knapp, Chem. Phys. 85 (1984) 73.
2. P. O. J. Scherer, S. F. Fischer, Chem. Phys. 86 (1984) 269.
3. S. Kurita, T. Honma, H. Nakamura, T. Sekiya, M. Nakajima, T. Suemoto, J. Lumin. 108 (2004) 15.
4. K. Miyasue, T. Honma, T. Sekiya, S. Kurita, M. Nakajima, T. Suemoto, J. Lumin. 112 (2005) 416.
Fig. 1 decay curve of the J-band emission











_1149327439.unknown

