Exciton luminescence of boron nitride nanotubes and nano-arches

B. Berzinaa, L. Trinklera, V. Korsaka, R. Krutohvostova, 

D. L. Carrollb, K. B. Ucerb, and R. T. Williamsb* 
aInstitute of Solid State Physics, University of Latvia, 8 Kengaraga Str., LV-1063 Riga, Latvia
bDepartment of Physics and Center for Nanotechnology and Molecular Materials, Wake Forest University, Winston-Salem, NC 27109 USA
We report photoluminescence (PL) and PL-excitation spectroscopy of BN nanotubes mixed with some residual h-BN starting material, and of h-BN microcrystalline powder.  The excitation spectroscopy [1] is crucial in distinguishing a prominent h-BN defect PL signature[2] from features possibly assignable to the nanotube phase.  The nanotube phase exhibits a broad-band PL near 380 nm, in agreement with cathodoluminescence from a sample comprising > 90% nanotubes.[3]  Detailed measurements on our nanotube sample show the broad PL spectrum around 380 nm to be a superposition of bands whose PL energy correlates with a distribution of excitation thresholds.  The thresholds are hypothesized to be band gaps of nanotubes having different radii.  According to calculations [4], smaller tube radius corresponds to smaller band gap.  We also observe 390-nm broad-band PL in spectra from microcrystalline h-BN.   It originates from the surfaces of the grains and is similar in many ways to the family of bands around 380 nm in nanotube-BN.  The 390-nm end of the distribution of nt-BN PL bands corresponds to the smallest radius of nanotube.   This caused us to wonder if there are high-curvature surface structures on h-BN microcrystals similar to nt-BN.   When rolled as a tube, the hexagonal BN sheets can form nanotubes (nt-BN).  Stacked as planes, the sheets become crystalline hexagonal boron nitride (h-BN), structurally similar to graphite.  The sheet edges comprising (1100) faces of h-BN and graphite terminate in dangling sp2 bonds that are susceptible to reconstruction.  A particular reconstruction that has been observed on both h-BN [5] and graphite is the nano-arch formed by bonding between adjacent sheet edges.  This reconstruction amounts to half-nanotubes lining the (1100) faces.  The tightest radii occur for single-wall arches between adjacent planes.  Nested arches similar to multiwall half-nanotubes also occur.  On this basis we expect similarities of electronic structure on reconstructed edges of h-BN and in nt-BN, in line with the PL data. 
We thank E. Shishonok for providing microcrystalline h-BN. 

* corresponding author e-mail:  williams@wfu.edu

References
1.  B. Berzina, L. Trinkler, R. Krutohvostov, R. T. Williams, D. L. Carroll, R. Czerw, and E. Shishnook, phys. stat. sol. (c) 2, 318-321 (2005).

2.   J. Wu, Wei-Qiang Han, W. Walukiewicz, J. W. Ager III, W. Shan, E. E. Haller, and A. Zettl, Nano Lett. 4, 647-650 (2004).
3.  Chunyi Zhi, Yoshio Bando, Chengchun Tang, Dmitri Golberg, Rongguo Xie, and Takashi Sekigushi, Appl. Phys. Lett. 86, 213110 1-3 (2005).

4.  G. Y. Guo and J. C. Lin, Phys. Rev. B 71, 165402-1-12 (2005).

5.  L. Nistor, V. Teodorescu, C. Ghica, J. Van Landuyt, G. Dinca, and P. Georgeoni, Diamond and Related Materials, 10, 1352-1356 (2001). 
