UV photon entanglement through biexcitonic states

Keiichi Edamatsua,b*, Goro Oohataa,c, Ryosuke Shimizub*
aResearch Institute of Electrical Communication, Tohoku University

bCREST, Japan Science and Technology Agency (JST)

cERATO Semiconductor Spintronics Project, JST

Entanglement is one of the key features to quantum info-communication technology. Although parametric down-conversion has been used so far to generate highly entangled pairs of photons, entangled photon sources using semiconductors are desired for practical applications [1-3]. We reported the first experimental evidence of the generation of UV entangled photons via biexcitons in a semiconductor (CuCl) crystal [4]. Here we show our recent experimental results that exhibit a higher degree of entanglement and demonstrate the violation of Bell's inequality. Figure 1 shows an example of polarization-correlation measurements of the photon pairs. We find clear polarization correlations for the coincidence signal at =0, in accordance with the theoretical prediction of the polarization-entangled state

[image: image1.wmf](

)

(

)

2

1

2

1

2

1

2

1

2

1

2

1

L

R

R

L

V

V

H

H

+

=

+

=

Y

 ,                         (1)
where |X(i (i=1, 2) denotes the polarization state (H: horizontal, V: vertical, L: left circular, and R: right circular) of each photon. The density matrix of the two-photon polarization state derived from quantum tomographic analysis exhibits the fidelity F=0.85 to the ideally entangled state (1), indicating that the generated photon pairs are highly entangled beyond the classical limit (F=0.5). We also evaluated Clauser-Horne-Shimony-Holt (CHSH) type Bell's inequality of our photon pair state. The obtained S-value was S=2.34(0.10>2, indicating that our state clearly violated the inequality. This is the first experimental demonstration of the violation of Bell's inequality by use of photon pairs generated directly from a semiconductor. 

[image: image2.emf]-50 0 50

Delay Time  (ns)

0

10

20

C

o

i

n

c

i

d

e

n

c

e

 

C

o

u

n

t

s

 

i

n

 

3

0

0

s

HH

-50 0 50

0

10

20

C

o

i

n

c

i

d

e

n

c

e

 

C

o

u

n

t

s

 

i

n

 

3

0

0

s

HV

-50 0 50

0

10

20

C

o

i

n

c

i

d

e

n

c

e

 

C

o

u

n

t

s

 

i

n

 

3

0

0

s

VH

-50 0 50

0

10

20

C

o

i

n

c

i

d

e

n

c

e

 

C

o

u

n

t

s

 

i

n

 

3

0

0

s

VV

-50 0 50

LL

LR

RL

RR


* corresponding author e-mail:  eda@riec.tohoku.ac.jp

References

1. S. Savasta, G. Martino, and R. Girlanda, Solid State Commun. 111, 495 (1999) 

2. C. Santori et al., Phys. Rev. B 66, 045308 (2002) 

3. R.M. Stevenson et al., Nature 439, 179 (2006) 

4. K. Edamatsu, G. Oohata, R. Shimizu and T. Itoh, Nature 431, 167 (2004)




�


 Fig. 1








_1209803876.unknown

