Photo-induced spin-state dynamics near the thermal phase transition temperature in the spin-crossover complex 
Hiroshi Watanabea, Azzedine Bousseksoub, and Koichiro Tanakaa
aDepartment of Physics, Graduate School of Science,  Kyoto University,  Kyoto, 606-8502, Japan
bLaboratoire de Chimie de Coordination, CNRS, UPR 8241, 31077 Toulouse, France
Recently photo-induced phase-transition phenomena have been attracting much attention around the thermal phase transition temperature in spin-crossover complexes. In this study, we investigate relaxation dynamics of photo-induced spin-state in the [Fe(ptz)6](BF4)2 compound by transient absorption spectroscopy. [Fe(ptz)6](BF4)2 shows a spin transition with hysteresis loop (T1/2↓=128K,T1/2↑=135K). The X-ray diffraction measurements reveal that spin transition is accompanied by the structural phase transition.[1] Figure 1 shows relaxation dynamics from photo-excited state(□) near the spin transition temperature. One can see 2-step relaxation via the intermediate state. As temperature increases, the interval of the state becomes faster and this state almost disappears at 122K. Above 122K, the intermediate state reappears and the interval of the state gets longer. The inset in Fig. 1 shows a summary of high spin-state dynamics. It is confirmed that high-spin fraction of the intermediate state increases abruptly at 122K, suggesting that the intermediate state may take a high-spin state or a low-spin state. A spin transition occurs between the two states at 122K. This suggests that the structure of the intermediate state has the same structure of the high temperature state which is different from photo-excited state(□) or final state(○).
[image: image1.emf]1.0

0.5

0.0

HS fraction

140 135 130 125 120 115

Temperature(K)

Fe(ptz)

6

(BF

4

)

2

final state (

○

)

intermediate state (

△

)

photo-excited state (

□

)

128

125 123

122

121 118

1.0

0.5

0.0

HS fraction

140 135 130 125 120 115

Temperature(K)

1.0

0.5

0.0

HS fraction

140 135 130 125 120 115

Temperature(K)

1.0

0.5

0.0

HS fraction

140 135 130 125 120 115

Temperature(K)

Fe(ptz)

6

(BF

4

)

2

final state (

○

)

intermediate state (

△

)

photo-excited state (

□

)

128

125 123

122

121 118


* corresponding author e-mail: hwata@scphys.kyoto-u.ac.jp
References  　[1] J. Kusz,P. Gutlich H. Spiering Top.Curr.Chem.234 (2004) 129.
Fig.1  Relaxation dynamics in  [Fe(ptz)6](BF4)2  from photo-excited(□) state to final state(○) through intermediate state(△) after photo-excitation stopped. Inset shows thermal dependence of HS fraction of these three state(△,○,□) and thermal hysteresis(+)








