Polarization-resolved degenerate four-wave mixing of CdS nanocyrstals in a nonresonant region
S. M. Maa, J. T. Seoa*, Q. Yanga, L. Creekmore a, R. Battle a, B. Tabibi a, and W. Yub
aDepartment of Physics, Hampton University, Hampton, VA 23668, U. S. A
bDepartment of Chemistry, Rice University, Houston, Texas 77005, U. S. A
The third-order nonlinear susceptibilities of various concentrations TOPO-passivated CdS nanocrystals were investigated using polarization-resolved degenerate four-wave mixing (DFWM) in a nonresonant excitation region. The average diameter of CdS nanocrystals was near 2.6 nm. The excitation light was 532 nm wavelength, 8 ns pulse width, and 10 Hz repetition rate. Figure 1 shows the absorption spectra of CdS nanocrystals and a strong blue shift of bandgap energy from the bulk state. Figure 2 shows the third-order nonlinear susceptibilities using the parallel and orthogonal DFWM.
	
[image: image1.wmf]300

400

500

600

0

1

2

3

4

l

ex

=532 nm

Absorbance

Wavelength (nm)

CdS Nanocrystals

Ab. Peak: ~387 nm

Av. Diameter: 2.6 nm

 C=1.60x10

-2

 mol/m

3

 C=1.26x10

-2

 mol/m

3

 C=8.22x10

-3

 mol/m

3

 C=4.85x10

-3

 mol/m

3

 C=1.71x10

-3

 mol/m

3


	
[image: image2.wmf]0.0

0.5

1.0

1.5

0.0

0.5

1.0

1.5

2.0

2.5

Concentration (10

-2

mol/m

3

)

CdS nanocrystals

 Parallel polarization

 Slope=1.41x10

-19

 

     

g

h

 

xxxx

~1.25x10

-42

 m

5

/V

2

 (~8.95x10

-29

 esu)

 Parallel polarization

 Slope=4.13x10

-20

     

g

h

 

xyyx

~3.66x10

-43

 m

5

/V

2

 (~2.62x10

-29

 esu)

     

g

h

xyyx

/

g

h

xxxx

=0.29

c

(3)

 (10

-21

 m

2

/V

2

)



	Figure 1:  Absorption spectra of CdS nanocrystals
	Figure 2:  The third-order susceptibilities of CdS nanocrystals


The second hyperpolarizabilities 
[image: image3.wmf]h

ijkl

g

 of the DFWMs were extracted from the slope of figure 2 and the ratio 
[image: image4.wmf]h

xxxx

h

xyyx

g

g

/

 was 0.29, which indicated a large contribution of electronic polarization process to the third-order nonlinearity of CdS nanocrystals.[1]
This work at Hampton University was supported by Army Research Laboratory (DAAD17-02-C-0107), Army Research Office (DAAD19-03-1-0011, W911NF-04-1-0393), National Science Foundation (EEC-0532472, HRD-0400041, PHY0139048), and Department of Energy (DE-FG02-97ER41035).
* corresponding author e-mail:  jaetae.seo@hamptonu.edu
References
1. H. S. Nalwa, Nonlinear optics of organic molecules and polymers, edited by  H. S. Nalwa and S. Miyata (CRC Press, Inc., 1997), p. 571
_1202635627.bin

_1202672590.bin

_1202633442.unknown

_1202633358.unknown

