Excitonic processes of lattice degradation in rare-gas solids

A. N. Ogurtsov*, N. Yu. Masalitina, O. N. Bliznjuk
National Technical University "KhPI", Frunse Street 21, Kharkov 61002, Ukraine

Rare-gas solids (RGS) are the model systems in physics and chemistry of solids, and a lot of information about their electronic excitations has been documented in several books and reviews (see e.g. Ref. 1 and references therein). Because of strong interaction with phonons the excitons and holes in RGS are self-trapped, and a wide range of electronic excitations are created in samples: free excitons (FE), atomic-like (A-STE) and molecular-like self-trapped excitons (M-STE), molecular-like self-trapped holes (STH) and electrons trapped at lattice imperfections. The trapping of excitons induces inelastic modification of RGS crystal lattice [1]. The subthreshold inelastic excitonically-induced atomic processes in RGS such as defect formation and desorption under excitation by photons and electrons with a kinetic energies below the threshold of knock-on of atoms from the lattice sites were studied recently [2]. However, to our knowledge, the kinetic analysis of the dose curves of excitonically-induced accumulation of crystal lattice imperfections in RGS was not done up to now. 

In the present paper we propose the simple kinetic model for excitonically-induced defect accumulation processes, using photoluminescence as a sensitive tool for real-time monitoring of the point defect concentration in RGS under irradiation. The experiments were carried out at the SUPERLUMI-station at HASYLAB, DESY, Hamburg. The process of defect accumulation may be written as consecutive process 
[image: image1.wmf]D

S

T

E

®

«

+

, where E is the mobile excitation (e.g. free exciton), which is trapped at trapping center T (e.g. lattice imperfection) and forms an excited metastable trapped center S (e.g. A-STE, or M-STE), which can be considered as metastable short-lived lattice defect. Radiative decay of the short-lived S-center either returns the lattice into the initial state without permanent defect, or forms the permanent defect D (Frenkel pair). The time dependence of luminescence intensity of 'defect' subband under steady-state conditions may be expressed in form: 
[image: image2.wmf]t

K

t

L

I

t

I

×

×

+

+

=

-

1

0

)

(

)

(

, where K and L are the specific constants expressed via the rate constants of elementary steps in the process; I0 is the initial intensity of 'defect' luminescence due to preirradiated defects. The results of fitting of time dependences of radiation-induced changes in photoluminescence excitonic spectra of solid Xe and Ne will be presented.

* corresponding author e-mail:  ogurtsov@kpi.kharkov.ua
References

1. A.N. Ogurtsov, Advances in Spectroscopy of Subthreshold Inelastic Radiation-Induced Processes in Cryocrystals, in: E.C. Faulques et al. (eds.), Spectroscopy of Emerging Materials, Kluwer Academic Publishers, Dordrecht, 2004.
2. Publications at  http://users.kpi.kharkov.ua/ogurtsov/ 

_1190997478.unknown

_1200645140.unknown

